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CIRCULAR
AMENDMENTS AND SUPPLEMENTS TO THE APPENDIX TO THE CIRCULAR NO. 05/2018/TT-BXD DATED JUNE 29, 2018 OF THE MINISTRY OF CONSTRUCTION ON INSTRUCTIONS FOR EXPORTATION OF MINERALS USED AS BUILDING MATERIALS

Pursuant to the Law on Minerals dated November 17, 2010; 
Pursuant to the Government's Decree No. 81/2017/ND-CP dated July 17, 2017, defining the functions, tasks, powers and organizational structure of the Ministry of Construction; 
Pursuant to the Government’s Decree No. 24a/2016/ND-CP dated April 5, 2016 on administration of building materials;
Pursuant to the Government's Decree No. 158/2016/ND-CP dated November 29, 2016 specifying and guiding the implementation of a number of articles of the Law on Minerals;
Pursuant to the Government's Decree No.69/2018/ND-CP dated May 15, 2018 elaborating on certain articles of the Law on Foreign Trade Management;
Upon the request of the Director of the Department of Building Materials; 
Minister of Construction hereby promulgates the Circular on amendments and supplements to the Appendix to the Circular No. 05/2018/TT-BXD dated June 29, 2018 of the Ministry of Construction on instructions for exportation of minerals used as building materials.
Article 1.
Circular No. 05/2018/TT-BXD dated June 29, 2018 of the Ministry of Construction on instructions for exportation of minerals used as building materials shall be amended and supplemented as follows: 

Replacing the Appendix I on List, technical specifications and indicators of minerals used as building materials for export by the Appendix I on List, technical specifications and indicators of minerals used as building materials for export to this Circular.

Article 2. Entry into force
This Circular shall enter into force on December 1, 2019. 
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APPENDIX I
LIST, TECHNICAL SPECIFICATIONS AND INDICATORS OF MINERALS USED AS BUILDING MATERIALS FOR EXPORT 
(To the Circular No. 05/2019/TT-BXD dated October 10, 2019 on amendments and supplements to the Appendix to the Circular No. 05/2018/TT-BXD dated June 29, 2018 of the Ministry of Construction on instructions for exportation of minerals used as building materials)
	HSS Code
	Description 
	Technical specifications and indicators

	I
	White silica sand, yellow molding sand
	 

	2505.10.00
	White silica sands used for production of building materials or in other industries
	Processed (screened, concentrated, washed or graded);

SiO2 content ≥ 97 %;

Particle size ≤ 1.0mm

	2505.90.00
	White silica sands used to make molds or in other industries  
	Processed (screened, concentrated, washed, graded, encapsulated or not encapsulated);

SiO2 content ≥ 95 %;

Particle size ≤ 2.5mm

	2505.90.00.90
	Yellow sand or sand made of crushed gravel, pebbles, quartzite, sandstone, quartz, etc., which is used to make moulds or in other industries    
	Processed (screened, concentrated, washed, graded, encapsulated or not encapsulated);

SiO2 content ≥ 85 %;

Particle size ≤ 2.5mm

	2505.10.00.10
	Fine or ultra-fine powder quartz (manufactured from white silica sand, quartz, quartzite) used to produce building materials or in other industries  
	Processed (screened, concentrated, washed, dried, crushed, graded);

SiO2 content ≥ 97 %;

Particle size ≤ 96 pm

	II
	Stone slabs
	 

	2515.12.20
	Marble and limestone cut by sawing or otherwise into tiling or paving slabs 
	Thickness ≤ 300 mm

	2516.12.20
	Granite, gabro, basalt and other stones cut by sawing or otherwise into tiling or paving slabs 
	Thickness ≤ 300 mm

	2516.20.20
	Sandstone cut by sawing or otherwise into tiling or paving slabs
	Thickness ≤ 300 mm

	2506.10.00
	Quartz cut by sawing or otherwise into tiling or paving slabs
	Thickness ≤ 300 mm

	2506.20.00
	Quartzite cut by sawing or otherwise into tiling or paving slabs
	Thickness ≤ 300 mm

	2514.00.00
	Slate manufactured by sawing or otherwise into tiling, paving or cladding slabs
	Thickness ≤ 50 mm

	6801.00.00
	Curbstones of natural stone (except slate)
	Thickness ≤ 300 mm

	6802.21.00
	Marble manufactured into tiling or paving slabs (with a flat or even surface)
	Thickness ≤ 300 mm

	6802.23.00
	Granite manufactured into tiling or paving slabs (with a flat or even surface)
	Thickness ≤ 300 mm

	6802.29.10
	Limestone manufactured into tiling or paving slabs (with a flat or even surface)
	Thickness ≤ 300 mm

	6802.29.90
	Other natural stones manufactured into tiling or paving slabs (with a flat or even surface)
	Thickness ≤ 300 mm

	III
	Stone blocks
	 

	2515.20.00.10
	White marble quarried, cut or sawed into flat blocks
	Volume ≥ 0.5 m3

	2515.12.10
	Marble, limestone and dolomite quarried, cut or sawed into flat blocks
	Volume ≥ 0.5 m3

	2516.12.10
	Granite, gabro, basalt, sandstone and other stone quarried, cut or sawed into flat blocks
	Volume ≥ 0.5 m3

	IV
	Stone sculptures
	 

	6802.91.10
	Stone sculpture made from marble
	Worked or sculpted into products

	6802.92.00
	Stone sculpture made from limestone
	Worked or sculpted into products

	6802.93.00
	Stone sculpture made from granite
	Worked or sculpted into products

	6802.99.00
	Stone sculpture made from other natural stones
	Worked or sculpted into products

	6802.10.00
	Setts, stones, lumps, granules, powder of natural stone and the like
	Worked or manufactured into products

	V
	Building stone
	 

	V-a
	Used for concrete aggregates, road metalling or other purposes
	 

	2517.10.00
	Pebbles, gravel or basalt, etc. used for concrete aggregates, road metalling or other purposes
	Crushed, ground or sieved into products in particle size ≤ 100mm 

	2517.49.00
	Limestone, granite, gabro, marble, sandstone, quartz and other stone used for concrete aggregates, road metalling and other purposes
	Crushed, ground or sieved into products in particle size ≤ 100 mm 

	V-b
	Used for embankments, footing, wall construction, sidewalks, road pavements or for other purposes
	 

	2515.11.00
	Other building stones (including freestone, ledgestone, etc.) made from marble, white marble or limestone used for embankments, footing or wall construction, sidewalks, road pavements and for other purposes 
	Worked, trimmed or cut into products

	2516.11.00
	Other building stones (including freestone, ledgestone, etc.) made from granite, gabro, basalt and other stones used for embankments, footing or wall construction, sidewalks, road pavements and for other purposes 
	Worked, trimmed or cut into products

	2516.20.10
	Other building stones (including freestone, ledgestone, etc.) made from sandstone used for embankments, footing or wall construction, sidewalks, road pavements and for other purposes 
	Worked, trimmed or cut into products

	2516.90.00
	Other monumental or building stone or stone used for other purposes 
	Worked, trimmed or cut into products

	2515.20.00
	Mosaic white marble cubes having a volume of less than 0.5 m3
	Worked, trimmed or cut into products

	VI
	Other minerals
	 

	2518.10.00
	Dolomite used for production of building materials or in other industries
	MgO content ≥ 18 %;

Particle size ≤ 100 mm

	2521.00.00
	Limestone used for the manufacture of lime or cement or in other industries
	Particle size ≤ 100 mm

	2507.00.00
	Kaolin used for production of building materials or in other industries
	Al2O3≥ 28%, Fe2O3 ≤ 1 %;

Particle size ≤ 0.2 mm

	2507.00.00
	Pyrophyllite kaolin used for production of building materials or in other industries
	Particle size ≤ 100 mm

	2508.30.00
	Fire clay used for production of building materials or in other industries
	Al2O3 ≥ 23 % ;

Particle size ≤ 0.2 mm

	2529.10.00
	Feldspar used for production of building materials or in other industries
	(K2O+Na2O) content ≥ 7%;

Particle size ≤ 100 mm


 
